Magnetic and transport properties of δ-Zn10Fe

D. Stanić1,2, P. Popčević1, J. Ivkov1, A. Smontara1,  M. Bobnar3, S. Vrtnik3,  M. Feuerbacher4, Z. Jagličić5, J. Dolinšek3

1Institute of Physics, Laboratory for the Study of Transport Problems, Zagreb, Croatia

2Department of Physics, J. J. Strossmayer University of Osijek, Osijek, Croatia

3J. Stefan Institute, University of Ljubljana, Ljubljana, Slovenia

4Institut für Festkörperforschung, Forschungszentrum Jülich, Jülich D-52425, Germany

5Institute of Mathematics, Physics and Mechanics, Ljubljana, Slovenia

We have studied magnetic susceptibility, electrical resistivity, thermoelectric power, thermal conductivity, specific heat and Hall coefficient of a phase (δ) that exists in Zn-rich part of Zn-Fe system. This phase crystallizes in hexagonal space group P63/mmc with unit cell parameters a=12.787(3) Å, c=57.222(7) Ǻ and 556 atoms in unit cell [1]. The sample was a single crystal and magnetic susceptibility measurements reveal that it is a paramagnet without any hysteresis in magnetization curve. The electrical resistivity amount to about 190 cm at the room temperature. It is a metallic like with relatively large residual resistivity at low temperatures and positive temperature coefficient, but tends to saturate at room temperature. Low-temperature specific heat in C/T versus T2 plot shows an increase in C/T below 8 K, that is frequently observed in heavy fermion systems. The thermoelectric power is small (<4 μV/K) and negative with complicated temperature behaviour (local minimum around 70 K an maximum around 150 K). The thermal conductivity is anomamalolously low (<10 W/mK) for an alloy of metallic elements. Hall coefficient is positive and increases significantly with temperature at lower temperatures, while exhibiting a tendency to saturate at temperatures above the room temperature. Such temperature behaviour could be attributed to the anisotropy of electron scattering times [2].

[1] C.H.E. Belin, R.C.H. Belin, J. Sol. Stat. Chem. 151 (2000) 85

[2] P. Popčević et al., Phys. Rev. B 81 (2010) p.184203.

Corresponding author e-mail: dstanic@ifs.hr

Poster presentation preferred